## Slide 1
Completely Alternating Copolymerization of CO2 and Epoxides to Polycarbonates
Donald J. Darensbourg
Texas A&M University, Department of Chemistry
djdarens@mail.chem.tamu.edu
+
+

## Slide 3
Greener Synthesis of Polycarbonates
No extraneous solvent required
100% atom economy
Constructive use of abundant “waste” C1 feedstock
Living polymerization
Typical Catalytic System: (salen)M(III)X with onium salt cocatalyst
Robust, tetradentate* ligand
Activity/Selectivity tunable by altering
R1, R2, R3, M, X
Darensbourg, D. J. Chem. Rev. 2007, 107, 2388-2410.
Darensbourg, D. J., Wilson, S. J. Green Chem. 2012, 14, 2665–2671..
Typical System: M = Cr, Co
R1 = R2 = tBu
R3 = -C2H4-, cyclohexyl
PPNX
nBu4NX

## Slide 4
ASI® ReactIR 1000
ReactIR™ ic10
Excellent for reactions run with at
least 12 mL at temperatures ≥ 25 oC.
Small high-pressure reactor designed in-house.
Manages well with small scale reactions (< 5 mL).
System can be heated or cooled to any practical temperature.
Attenuated Total Reflectance
Infrared Spectroscopy
argon,
vacuum
CO2 inlet
reactants inlet
probe
reactants inlet
//
//
argon,
vacuum
CO2 inlet
jacketed heating mantle
crystal
Monitoring Polymerization Kinetics – in situ ATR FT-IR
1750 cm-1
Wavenumbers(cm-1)
1802 cm-1
1810 cm-1
Time
Solution becomes too viscous at this point.
Time (h)
Absorbance

## Slide 5
Coupling Mechanism
See review: Darensbourg, D. J.; Yeung, A. D.
Polymer Chemistry 2014, 5, 3949—3962.

## Slide 6
Routes to Cyclic Carbonates
Metal free pathway has much lower kinetic barrier.

## Slide 7
Copolymerization of Styrene Oxide and Carbon Dioxide
PPNX as cocatalyst
Thermal stability up to 300 oC and Tg = 80 oC
25 oC, TOF = 75 h-1 @ 2.0 Mpa CO2 Selectivity PSC:SC of 99:1
Wu, G.-P.; Wei, S.-H.; Lu, X.-B.; Ren, W.-M.; Darensbourg, D. J. Macromolecules 2010, 43, 9202.
Wu, G.-P.; Wei, S.-H.; Ren, W.-M.; Lu, X.-B.; Li, B.; Zu, Y.-P.; Darensbourg, D. J. Energy & Environmental Sci. 2011, 4, 5084-5092.

## Slide 8
Rapid and Reversible Chain Transfer Processes
Bimodal Distribution of Molecular Weights
Mn (g/mol)
16800
11000
6800
4200
(0 equiv H2O)
(5 equiv H2O)
(10 equiv H2O)
(20 equiv H2O)

## Slide 9
Polyether Polyols
http://www.econic-technologies.com/technologies/products/polyols/
Automotive
Adhesives,
Sealants &
Binders
Coatings &
Elastomers
Building &
Construction
Polyols currently used derived 100% from petroleum resources (polyethers).
Replaced with polycarbonate polyols derived in part (~50%) from CO2.
Appliances
Footwear
Feedstocks

## Slide 10
Desired Properties
Seong, J.E.; Na, S.J.; Cyriac, A.; Kim, B.-W.; Lee, B.Y. Macromolecules. 2010, 43, 903-908.
BPA Polycarbonate
Lexan®
Industrial standard polycarbonate
Tg ≈ 150 oC
Amorphous, robust polymer
High Mn’s achievable
Chain entanglement at low MW
Wu, G.-P.; Wei, S.-H.; Lu, X.-B.; Ren, W.-M.; Darensbourg, D.J. Macromolecules 2010, 43, 9202-9204.
poly(propylene carbonate)
Tg ≈ 40 oC
excellent mechanical properties
industrially produced
poly(cyclohexene carbonate)
Tg ≈ 115 oC
easy to polymerize
brittle polymer
poly(styrene carbonate)
Tg ≈ 80 oC
sensitive polymerization
poly(1-hexene carbonate)
Tg ≈ -15 oC
?
What conditions can we use to
produce polymers similar
to that of BPA polycarbonate?
high glass transition temperature (Tg)
Our Focus:

## Slide 11
Td ~ 249 oC
Poly(indene carbonate)
Tg around 140 oC
Highest reported Tg
for CO2/epoxides coupling!
Coupling of CO2 and Indene Oxide
Stephanie Wilson
Darensbourg, D.J.; Wilson, S. J. J. Am. Chem. Soc. 2011, 133, 18610-18613.

## Slide 12
Binary vs Bifunctional Catalyst Systems
versus
Selectivity for Polymer
(1)
(2)
polymer
cyclic
(1)
(2)
Darensbourg, D.J.; Wilson, S. J. Macromolecules 2013, 46, 5929.

## Slide 13
Bifunctional Catalyst System – How They Work
≡
polymer detaches
backbiting to
cyclic commences
polymer attracted
to ammonium cation
backbiting prevented
CO2,

## Slide 14: Design of New Polymeric Materials
Terpolymerization, addition of a second epoxide monomer.
Postfunctionalization of copolymers.
Diblock polymers incorporating ROP of other cyclic monomers, e.g., polycarbonate-polylactide
(NOTE: polylactides are among the few biodegradable polymers with FDA approval for human clinical use. Controlled drug delivery and tissue engineering scaffolds.)

## Slide 15: Terpolymerization with Postpolymerization Functionalization
Using free-radical initiator (AIBN), add

## Slide 16
Postfunctionalization of Copolymers Hybrid Polymers
Darensbourg, D. J.; Tsai, F.-T., Macromolecules, 2014, 47, 3806—3813.

## Slide 17
uv
uv
cat.
terpolymerization
crosslinking
surface
functionalization
Functionalization of Polycarbonate Films
or

## Slide 18
Tandem Synthesis of Poly(styrene carbonate-block-lactide)
Wu, G.-P.; Darensbourg, D. J.; Lu, X.-B. J. Am. Chem. Soc., 2012, 134, 17739-17745.
Cyclic styrene carbonate
Poly(styrene carbonate)
PSC-block-PLA
Lactide
Cyclic styrene carbonate

## Slide 19
A One-Pot Synthesis of a Triblock Copolymer
from PO/CO2 and Lactides
Darensbourg, D. J.; Wu, G.-P. Angew. Chem. Int. Ed. 2013, 52, 10602-10606.
HO-(PPC)-OH
PLA-b-PPC-b-PLA

## Slide 20
ABA Triblock Polymers

## Slide 21
Darensbourg, D. J.; Chung, W.-C.; Wang, K.; Zhou, H.-C. ACS Catalysis, 2014, 4, 1511–1515.

## Slide 22
Acknowledgements
DJD Group Members:
Wan-Chun Chung
Samuel Kyran
Andrew Yeung
Yanyan Wang
Dr. Fu-Te Tsai
Dr. Rongjiao Zhu
Dr. Hamidreza Samouei
Former DJD Group Members:
Dr. Sheng-Hsuan Wei
Dr. Stephanie Wilson
Dr. Ross Poland
Dr. Osit Karroonnirun
Dr. Adriana Moncada
Dr. Wonsook Choi
Dr. Eric Frantz
Dr. Shawn Fitch
Dr. Jeremy Andreatta
Dr. Carla Rodarte
Dr. Adolfo Horn Jr.
Dr. Binyuan Liu
Dr. Bo Li
Dr. Guangpeng Wu